SP00591  (Special Provisions for the 2021 Book) 	(Bidding on or after: 12-01-20

Last updated: 08-19-20

This Section requires SP00504)

# SECTION 00591 - SPRAY WATERPROOFING MEMBRANE

(Follow all instructions and make all edits with “Track Changes” turned on. This Section is not published in the Oregon Standard. If there are no instructions [orange text] above a subsection, paragraph, sentence, or bullet, then include it in the project, unless the item(s) that are included in the subsection, paragraph, sentence, or bullet are not required on the Project and then they should be deleted. In general do not re-number or re-letter subsections when item(s) are deleted. Delete all orange text before preparing the final document. All other modifications to this Section will require ODOT Technical Resource and State Specifications Engineer approval.)

Section 00591, which is not a Standard Specification, is included in this Project by Special Provision.

## Description

00591.00  Scope - This Work consists of furnishing and placing spray waterproofing membrane on bridge decks as shown.

00591.02  Submittals - Submit the following at least 7 Calendar Days before the pre placement conference:

The manufacturer’s product data sheet

The manufacturer’s written installation instructions

A Material Safety Data Sheet for each primer and epoxy polymer component

Manufacture dates and shelf-life expiration dates for each production lot of primer and epoxy polymer components

Tabulated data indicating the estimated cure time, in minutes, for the allowable ambient temperature range, in increments of 10 °F, for both the primer and polymer membrane

A detailed work plan for the membrane preparation, application, and cleanup

The Manufacturer’s recommended application rate, square feet per gallon, to achieve a minimum membrane thickness of 3/16 inch

Names of manufacturer-approved supervisory personnel meeting the requirements of 00591.30

For each spray membrane proposed for use, submit for the Engineer's review a manufacturer approved procedure for preparing the deck surface, applying the membrane, and placing the Aggregate surface. Include in the procedure the identification of the manufacturer's representative, the number of persons required, Equipment, installation sequence, traffic control, and the estimated time schedule for installing the membrane and opening the Bridge to traffic.

For Bridges with curbs or concrete rails, submit unstamped manufacturer Working Drawings according to 00150.35, detailing membrane placement at the curbs or rail.

00591.04  Pre-Placement Conference - Hold a pre-placement conference with the Contractor's supervisory personnel, the manufacturer's authorized representative, the manufacturer certified applicator(s), and the Engineer at least 14 Calendar Days before applying each membrane.

## Materials

00591.10  Materials - Furnish a warranted spray waterproofing membrane system that complies with the maximum profile grades and superelevations shown. Profile grade and superelevation limitations for products are listed in the QPL and are available from the manufacturer.

(a)  Primer - Furnish a primer from the QPL.

(b)  Spray Membrane - Furnish spray waterproofing membrane from the QPL.

(c)  Broadcast Aggregate - Furnish broadcast Aggregate from section 00556.10(b) of the QPL.

(d)  Tack Coat - Furnish PG 64-22, PG 70-22, PG 64-28 or PG 70-28, hot asphalt cement tack coat or a tack coat as part of the waterproof membrane system from the QPL. Do not use an emulsified tack.

(e)  Handling Materials - Store spray waterproofing membrane at a temperature between 55 °F and 95 °F or as recommended by the manufacturer, whichever is more restrictive.

## Labor

00591.30  Manufacturer's Representative - Provide the services of a manufacturer's representative authorized to observe the installation of each membrane system, including the ACP wearing Course. The manufacturer's representative shall be an employee of the membrane system manufacturer. Do not begin membrane Work until the manufacturer's representative is on site and authorizes the Work to begin.

Follow the recommendations of the manufacturer's representative when installing the spray membrane system, as provided in this Section. Instruct the manufacturer's representative to alert the Contractor and the Engineer of anything that could affect the performance of the spray waterproofing membrane or the warranty.

Submit a daily written report to the Engineer that has been prepared by the manufacturer's representative and details all membrane-related activities, test results, observations, repairs, post-spray survey results, tack coat timing issues, and contaminated tack repairs. Submit the daily written report by the end of each business Day until the Work is complete.

00591.31  Applicator Qualifications - Provide manufacturer authorized applicators. Applicators shall be re-certified yearly by the manufacturer.

## Construction

00591.40  Construction -

(a)  General - Do not begin membrane installation until all Materials and Equipment necessary to perform the installation and required repairs, and qualified personnel are at the Project Site.

(b)  Application Conditions - Apply the spray waterproofing membrane on prepared surfaces when the following conditions are met:

The deck surface has been visually dry for at least 72 hours.

The ambient temperate and deck surface temperature are between 50 °F and 90 °F.

The deck surface temperature is at least 5 °F above the dew point.

No rain is forecasted for the duration of the membrane installation.

00591.41  Preparing Bridge Decks - Prepare all surfaces that are to be in contact with the spray waterproofing membrane according to Section 00504.

00591.42  Installation - After preparation Work has been approved by the manufacturer's representative, install spray waterproofing membrane according to the following:

Spray, squeegee, or roll primer at a rate of 1 gallon per 100 to 200 square feet of surface area or as recommended by the manufacturer.

Spray membrane over primed surfaces at a minimum rate of 1 gallon per 20 square feet of surface area, or as recommended by the manufacturer, to achieve a minimum thickness of 80 mils. Apply the spray membrane using methods recommended by the manufacturer.

In the presence of the Engineer, perform a post-spray survey of the membrane by chain drag sounding, infrared imaging or other approved methods to locate any delamination, bubbles, or other defects. Repair all defects in a manner consistent with the manufacturer’s recommendations and satisfactory to the Engineer and document on the daily written report.

Apply the Aggregate Surface according to one of the following methods:

Apply a polyurea Aggregate surface with broadcast Aggregate to the existing polyurea membrane surface. Spray the polyurea wearing surface at a thickness of 30 to 40 mils. Before the polyurea wearing surface sets, broadcast Aggregate to refusal to achieve at least 95 percent coverage. The polyurea, Aggregate, and application procedure shall be according to the manufacturer's recommendations.

Apply an epoxy Aggregate surface with broadcast Aggregate to the existing polyurea membrane surface. Apply the broadcast Aggregate to refusal to achieve at least 95 percent coverage. The epoxy, Aggregate and application procedure shall be according to the manufacturer’s recommendations.

Prior to applying the tack coat, thoroughly clean the Aggregate surface using blowers, brooms, vacuums, pressure washers or other methods to achieve a clean, dry surface.

Apply a tack coat before paving. Pave over tack within 4 hours of tack placement, or sooner if recommended by the manufacturer.

Traffic will be allowed on the Aggregate surface for 7 Calendar Days or as recommended by manufacturer, whichever is less, before beginning paving operations.

The manufacturer's representative shall accept each layer of the waterproofing membrane system, including the ACP wearing Course, before application of the next layer is allowed.

00591.46  Primer Bond Test - Before placing the membrane, test prepared surface to primer bond according to ASTM D4541, Method E, using Type V tester and 20 mm dollies. Unless otherwise directed, randomly select test locations with a minimum of one test per 750 square feet.

Minimum bond strength is 175 psi or substrate failure.

00591.47  Dry Film Thickness Test - Test spray membrane dry film thickness using test methods approved by the Engineer. Unless otherwise directed, randomly select test locations with a minimum of one test per 750 square feet.

00591.48  Membrane System Bond Test - Before allowing paving or traffic on the membrane, test the full depth membrane system according to ASTM D4541, Method E using Type V tester and 50 mm test dollies. Minimum bond strength is 175 psi or substrate failure. Cut 2 inch diameter cores full depth through the Aggregate Surface and 1/4 inch into concrete substrate. Unless otherwise directed, randomly select test locations with a minimum of one test per 750 square feet. Repair core holes with matching membrane system Materials.

00591.75  Manufacturer Warranty - Furnish a manufacturer warranty that unconditionally warrants to the Agency the product(s) and installation under this Section against failure, according to this subsection and 00170.85(c)(1). Use Agency-supplied warranty forms, available from the Engineer.

"Unconditionally warrant" means that the warranty covers all failures, regardless of the source or cause of the failure, including, without limitation, whether the source or cause is or may be related to workmanship, inspection, or choice of materials.

The Agency inspection of any portion of the Work during the Contract and during the product installation, the Agency acceptance of the Work, corrections under the warranty, or expiration of the warranty shall not relieve the obligations under this warranty.

(a)  Warranty Period - The warranty period shall be for 2 years.

(b)  Failure - For purposes of the warranty, failure is defined as:

Leakage of the membrane, or

Delamination of the membrane from the substrate or overlying Pavement.

(c)  Remedy - Upon notification by the Engineer of a failure as defined above, provide the following remedy at no additional cost to the Agency:

Submit a detailed repair plan to the Engineer for approval within 14 Calendar Days.

Unless otherwise approved in writing by the Engineer, complete permanent repairs within 60 Calendar Days. Until permanent repairs are completed and accepted, complete temporary repairs as required by the Engineer.

Use Materials and procedures meeting these Specifications.

Match repairs to finished grade.

Coordinate timing of repair Work with the Engineer.

(d)  Traffic Control; Agency's Right to Make Repairs - If, in the opinion of the Engineer, a failure causes or may cause a hazard, the failure may be temporarily corrected by Agency or other forces at no additional cost to the Agency. Replace temporary repairs with permanent repairs at no additional cost to the Agency, according to the Specifications, and within the time specified in 00591.75(c).

## Measurement

00591.80  Measurement - The quantities of spray waterproofing membrane will be measured on the area basis, and will be the sealed surface area, and will be limited to the Neat Lines and dimensions shown or directed.

Removal of existing asphalt wearing surfaces will be measured according to 00503.80.

## Payment

00591.90  Payment - The accepted quantities of spray waterproofing membrane will be paid for at the Contract unit price, per square foot, for the item "Warranted Spray Waterproofing Membrane".

Payment will be payment in full for furnishing and placing all Materials, and for furnishing all Equipment, labor, and Incidentals required to complete the Work as specified.

Payment for Work done under this Section will be limited to 75 percent of the amount due until the Agency has received the required manufacturer representative’s written reports and the signed manufacturer's warranty.

Removal of existing asphalt wearing surfaces will be paid for according to 00503.90.