SP00412  (Special Provisions for the 2021 Book) 	(Bidding on or after: 06-01-23

Last updated: 02-22-23

This Section requires SP00410

when 00412 is listed in Table 00410-1)

SECTION 00412 - CURED-IN-PLACE PIPE LINING

This Section title is replaced with the following:

# SECTION 00412 - CURED-IN-PLACE PIPE LINING THERMO CURE

(Follow all instructions and make all edits with “Track Changes” turned on. If there are no instructions [orange text] above a subsection, paragraph, sentence, or bullet, then include it in the project. Delete all orange text before preparing the final document. All other modifications to this Section will require ODOT Technical Resource and State Specifications Engineer approval.)

Comply with Section 00412 of the Standard Specifications modified as follows:

00412.00  Scope - Replace this subsection, except for the subsection number and title, with the following:

This Work consists of rehabilitating existing pipes by furnishing and installing pipe liners by cured-in-place pipe (CIPP) lining methods as shown using a thermosetting resin cured with hot water or steam.

00412.01 Submittals - Replace the paragraph beginning “Submit the following at least…” with the following:

Submit the following at least 10 Calendar Days before the preconstruction conference. List each submittal in a table of contents including a corresponding page number.

Replace the bullet beginning “Certification of test results…” with the following bullet:

Independent third party certification of test results confirming the CIPP liner system meets the minimum chemical resistance requirements according to ASTM F1216 and ASTM F1743 when lining storm sewers, sanitary sewers, industrial applications or as directed.

Add the following paragraph before the sentence beginning “Upon liner system…

Submit the following for approval according to 00150.37 at least 10 Calendar Days before ordering tube(s):

Verify Pipe length, rise and span, for each installation according to Section 00415 and include the corresponding tube size that will be ordered for each installation according to 00412.10. Do not order Material(s) until approval has been received.

(Use the following subsection .02 to list the CIPP design parameters. Obtain the parameter information from the Designer.)

00412.02  Design Parameters - Add the following to the end of this subsection:

Height of fill from invert	_________

Groundwater Elevation above invert	 _____

(Use the following line when chemical resistance parameters are required)

Chemical Resistance (ASTM F1216, ASTM F1743)	 _____

00412.70  General - Replace this subsection, except for the subsection number and title, with the following:

Ensure the cured liner is continuous and free from visual defects such as foreign inclusions, dry spots, pinholes, delamination, and wrinkles at all locations. Verify the lining is impervious and free of any leakage from water infiltration into the lined pipe or exfiltration from the lined pipe.

Cut both ends of the cured liner flush at the inlet and outlet points of the pipe, and seal with an epoxy or resin mixture compatible with the liner/resin system, providing a watertight seal.

Remove any temporary dams or filtration measures after Work is complete and pipe is clean and restored.

00412.71  Post Installation Video Inspection - Replace this subsection, except for the subsection number and title, with the following:

After installation of the CIPP perform a post-installation video inspection of the pipe according to Section 00415.

(Use the following subsection .80 when SP00410 is used and Section 00412 is listed as an option in Table 00410-1.)

00412.80  Measurement - Replace this subsection, except for the subsection number and title, with the following:

CIPP Liner and Service Line Reconnections will be measured according to 00410.80.

(Use the following subsection .90 when SP00410 is used and Section 00412 is listed as an option in Table 00410-1.)

00412.90  Payment - Replace this subsection, except for the subsection number and title, with the following:

CIPP Liner and Service Line Reconnections will be paid for according to 00410.90.