SP00413  (Special Provisions for the 2021 Book) 	(Bidding on or after: 06-01-23

Last updated: 02-22-23

This Section requires SP00410

when 00413 is listed in Table 00410-1)

SECTION 00413 - GRP CURED-IN-PLACE PIPE LINING & UV CURE

This Section title is replaced with the following:

# SECTION 00413 - GRP CURED-IN-PLACE PIPE LINING UV CURE

(Follow all instructions and make all edits with “Track Changes” turned on. If there are no instructions [orange text] above a subsection, paragraph, sentence, or bullet, then include it in the project. Delete all orange text before preparing the final document. All other modifications to this Section will require ODOT Technical Resource and State Specifications Engineer approval.)

Comply with Section 00413 of the Standard Specifications modified as follows:

00413.01 Submittals - Replace the paragraph beginning “Submit the following at least…” with the following:

Submit the following at least 10 Calendar Days before the preconstruction conference. List each submittal in a table of contents including a corresponding page number

Replace the bullet beginning “Independent third party certification…” with the following bullet:

- Independent third party certification of test results confirming that the CIPP liner system meets the initial structure properties according to ASTM F2019.

Add the following bullet after the bullet beginning “Independent third party certification…”:

- Independent third party certification of test results confirming that the CIPP liner system meets the minimum chemical resistance requirements according to ASTM F2019 and ASTM D5813 Section 6.4, when lining storm sewers, sanitary sewers, industrial applications or as directed.

Add the following paragraph to the end of this subsection:

Submit the following for approval according to 00150.37 at least 10 Calendar Days before ordering tube(s):

Verify Pipe length, rise and span, for each installation according to Section 00415 and include the corresponding tube size that will be ordered for each installation according to 00413.10. Do not order Material(s) until approval has been received.

(Use the following subsection .02 to list the GRP CIPP design parameters. Obtain the parameter information from the Designer.)

00413.02  Design Parameters - Add the following to the end of this subsection:

Height of fill from invert	_________

Groundwater Elevation above Invert	_________

(Use the following line when chemical resistance parameters are required)

Chemical Resistance (ASTM F1216, ASTM F1743)	 _____

(Use the following subsection .80 when SP00410 is used and Section 00413 is listed as an option in Table 00410-1.)

00413.80  Measurement - Replace this subsection, except for the subsection number and title, with the following:

CIPP Liner will be measured according to 00410.80.

(Use the following subsection .90 when SP00410 is used and Section 00413 is listed as an option in Table 00410-1.)

00413.90  Payment - Replace this subsection, except for the subsection number and title, with the following:

CIPP Liner will be paid for according to 00410.90.