SP00596A  (Special Provisions for the 2021 Book) 	(Bidding on or after: 06-01-23

Last updated: 02-28-23

This Section requires SP00440,

SP02001, SP02320 and SP02690)

# SECTION 00596A - MECHANICALLY STABILIZED EARTH RETAINING WALLS

(Follow all instructions and make all edits with “Track Changes” turned on. If there are no instructions [orange text] above a subsection, paragraph, sentence, or bullet, then include it in the project. Delete all orange text before preparing the final document. All other modifications to this Section will require ODOT Technical Resource and State Specifications Engineer approval.)

Comply with Section 00596A of the Standard Specifications modified as follows:

(Use the following subsection .01 and bullets when the contractor will be required to select a permanent proprietary MSE wall system. For "Bridge" retaining walls and "Highway" retaining walls, fill in the blank with the structure number. If the retaining wall does not have a structure number, delete the phrase ", structure no. ____ ,".)

00596A.01  Proprietary MSE Walls - Add the following to the end of this subsection:

Select one of the following preapproved proprietary MSE retaining wall systems for the wall, structure no. ____, as shown:

(Fill in the blanks with the proprietary retaining wall system name (including the "" symbol), company name and telephone number from the ODOT Geotechnical Design Manual, appendix 15-D.)

_________________________________________ MSE Retaining Wall System, provided by _________________________________ , telephone: ____________ .

_________________________________________ MSE Retaining Wall System, provided by _________________________________ , telephone: ____________ .

_________________________________________ MSE Retaining Wall System, provided by _________________________________ , telephone: ____________ .

(Use the following subsection .04(b) to list proprietary wall geotechnical and seismic design parameters. Obtain information from the designer. Delete what does not apply. Delete the language in orange parentheses that does not apply and delete all orange parentheses. Copy and paste the structure number, station limits, and associated bullets for each separate retaining wall.)

00596A.04(b)  Design Calculations - Add the following to the end of this subsection:

The following retaining wall design parameters have been established for this Project:

Structure No. _________ : Sta. _______ to Sta. ________ (Lt.)(Rt.)

Foundation soil unit density	 _________ lbs./cu. ft.

Foundation soil angle of internal friction	 _________ degrees

Foundation soil nominal (unfactored)

bearing resistance	 _________ lbs./sq. ft.

Retained soil unit density	 _________ lbs./cu. ft.

Retained soil angle of internal friction	 _________ degrees

Reinforced soil unit density	 _________ lbs./cu. ft.

Reinforced soil angle of internal friction	 _________ degrees

Peak ground acceleration coefficient (PGA)	 _________

Short period spectral acceleration coefficient (SS).	 _________

Long period spectral acceleration coefficient (S1)	 _________

Site class	 _________

Peak seismic ground acceleration coefficient

modified by zero period site factor (As)	 _________

Horizontal seismic acceleration coefficient (kh)	 _________

(Use the following bullet and sub-bullet when the Mononabe-Okabe method is not required. Repeat as necessary for variations in wall height and backslope along the wall.).

Between Station ______ and Station ______ (Lt.)(Rt.):

Total (static plus seismic) external

- seismic thrust (PAE) 	 __________ lbs./ft.

(Use the following bullet and sub-bullets to specify minimum length of soil reinforcement. Repeat as necessary for variations in wall height, backslope, bearing resistance and other parameters which can change along the wall.)

Between Station ______ and Station ______ (Lt.)(Rt.):

Minimum length of soil reinforcement

- for overall stability 	 ________ft.

Minimum length of soil reinforcement

- for external stability 	 ________ft.

00596A.11(c)  Modular Block Core and Drainage Backfill - Replace this subsection, except for the subsection number and title, with the following:

Furnish 3/4" - No. 4 PCC Aggregate Material meeting the requirements of 02690.20(a) through (e).

(Use the following subsection .12(e)(1) when precast concrete panel facing is required. Use one of the following options as instructed below. Delete the option that does not apply.)

00596A.12(e)(1)  Portland Cement Concrete - Add the following paragraph to the end of this subsection:

[ Option 1 - Use the following paragraph when an ARES™ wall system is not specified. ]

Furnish Class 4000 structural concrete meeting the requirements of Section 02001.

[ Option 2 - Use the following paragraph when an ARES™ wall system is specified. ]

For ARES™ retaining wall systems, furnish Class 4500 structural concrete meeting the requirements of Section 02001, except the maximum water-cementitious material ratio shall not exceed 0.44. For all other retaining wall systems use Class 4000 structural concrete meeting the requirements of Section 02001.

00596A.15  Elastomeric Bearing Pads for Precast Concrete Facing Panels - Replace this subsection, except for the subsection number and title, with the following:

In horizontal and diagonal joints between precast concrete panels, furnish the grade, size, number and type of bearing pads shown in the stamped Working Drawings and design calculations prepared by the manufacturer. Determine the stiffness, size, and number of bearing pads so that the final joint opening is 3/4 inch ± 1/8 inch or as shown.

(Use the following subsection .16 when KeySystem I TM, LANDMARKTM, or MESATM wall systems are specified in 00596A.01.)

00596A.16  Concrete Modular Block Facing Connection Devices - Add the following to the end of this subsection:

(Use the following paragraph when the KeySystem I TM wall system is specified.)

For KeySystem I TM wall systems, furnish connection pins that conform to AASHTO M 32 and are galvanized after fabrication according to AASHTO M 111.

(Use the following paragraph and table when the LANDMARKTM wall system is specified.)

For LANDMARKTM wall systems, furnish lock bars that are made of a rigid, polyvinyl chloride polymer conforming to the following requirements:

Property	Limits	Specification

Specific Gravity	1.4 (min.)	ASTM D792

Tensile Strength (at yield)	2,700 psi (min.)	ASTM D638

(Use the following paragraphs and tables when the MESATM wall system is specified.)

For MESATM wall systems, furnish block connectors for block courses with geogrid reinforcement that are glass fiber reinforced, high density polypropylene conforming to the following minimum material requirements:

Property	Limits	Specification

Polypropylene: Group 1,	73% ± 2%	ASTM D4101

Class 1, Grade 2

Fiberglass Content	25% ± 3%	ASTM D2584

Carbon Black	2% (min.)	ASTM D4218

Specific Gravity	1.08 ± 0.04	ASTM D792

Tensile Strength (at yield)	8,700 psi ± 1,450 psi	ASTM D638

Melt Flow Rate	(0.37oz. ± 0.16 oz.)/10 minutes	ASTM D1238

For MESATM wall systems, furnish block connectors for block courses without geogrid reinforcement that are glass fiber reinforced, high density polyethylene (HDPE) conforming to the following minimum material requirements:

Property	Limits	Specification

HDPE: Type III,	68% ± 3%	ASTM D1248

Class A, Grade 5

Fiberglass Content	30% ± 3%	ASTM D2584

Carbon Black	2% (min.)	ASTM D4218

Specific Gravity	1.16 ± 0.06	ASTM D792

Tensile Strength (at yield)	8,700 psi ± 725psi	ASTM D638

Melt Flow Rate	(0.11 oz. ± 0.07 oz.)/10 minutes	ASTM D1238

(NOTES to Specification Writer:

(1) The bid item quantity for MSE retaining walls is “Lump Sum,” and includes all labor, materials, and inclusive items necessary to complete the work. Items such as excavation, shoring, reinforced backfill, and standard copings are considered inclusive items to the wall pay item.

Items such as sidewalk copings, traffic barrier, moment slabs, guardrail and fencing are considered appurtenances along with the following items and should be included as separate bid items:

Items associated with project specific details such as architectural treatments, geomembrane barriers.

Items associated with incidental work, such as scour protection, dewatering, or foundation improvement, and items that cost more than 5 percent of the lump sum cost.

(2) For proprietary retaining wall systems, where details of wall construction are generally not known until after the construction contract is awarded, do not include estimated quantities for inclusive items.)

00596A.80  Measurement - Add the following to the end of this subsection:

The estimated quantities of retaining walls are:

(Provide wall area below. The wall area is bounded by the beginning and end of the wall, top of the wall (excluding wall coping), and top of the footing or leveling pad. If no footing or leveling pad exists, the bottom of the wall is used. Copy and paste more lines, as necessary, to list estimated areas for each retaining wall.)

Structure Number ____________ :

Station Limits	Area

Sta. ______ to Sta. ______ (Lt.)(Rt.)	___(Wall area here)___ sq. ft.

(Use the following paragraph to list estimated quantities for nonproprietary retaining wall systems only. Ensure that the Wall (Bridge) Designer provides estimated quantities for all-inclusive items such as excavation, shoring, reinforced backfill, leveling pads, wall drainage backfill/geotextile, and standard coping. Copy and paste more lines, as needed, to list estimated quantities for each nonproprietary retaining wall.)

The estimated quantities of listed Materials are:

Structure No. ______: Sta. ______ to Sta. ______ (Lt.)(Rt.)

Material	Estimated Quantities

________	____ cu. yd.

________	____ foot

________	____ lb.