SP00869  (Special Provisions for the 2021 Book) 	(Bidding on or after: 12-01-20

Last updated: 08-19-20)

# SECTION 00869 - CURB AND NON-TRAVERSABLE MEDIAN MARKINGS

(Follow all instructions and make all edits with “Track Changes” turned on. This Section is not published in the Oregon Standard. If there are no instructions [orange text] above a subsection, paragraph, sentence, or bullet, then include it in the project, unless the item(s) that are included in the subsection, paragraph, sentence, or bullet are not required on the Project and then they should be deleted. In general do not re-number or re-letter subsections when item(s) are deleted. Delete all orange text before preparing the final document. All other modifications to this Section will require ODOT Technical Resource and State Specifications Engineer approval.)

Section 00869, which is not a Standard Specification, is included in this Project by Special Provision.

## Description

00869.00  Scope - In addition to the requirements of Section 00850, 00860, and 00865, install curb markings and non-traversable median markings according to the following Specifications.

## Labor

00869.31  Manufacturer-Certified Installers - Provide certified installers according to 00850.31 for thermoplastic applications.

## Construction

00869.45  Installation - Apply curb markings and non-traversable median markings only when the following conditions are met:

The ambient temperature is at least 50 °F and rising

The pavement has been dry for at least 48 hours

30 Calendar Days of cure time for new concrete curb or median.

Apply the Material to the pavement according to the manufacturer’s installation instructions to the full height and width of curb or median as shown in the Plans.

Apply one or more of the following marking material types:

Paint - Apply according to 00860.45 along full height of curb face and along full width of top of curb or non-traversable median.

Thermoplastic, Sprayed - Apply according to 00865.45, using Method B Spray Markings to the full height of curb face and along full width of top of curb or non-traversable median.

Apply each application of painted thermoplastic marking at a thickness of 60 mils.

## Measurement

00869.80  Measurement - The quantities of non-traversable median markings will be measured on the area basis. The quantities of curb markings will be measured on the length basis.

## Payment

00869.90  Payment - The accepted quantities of Work performed under this Section will be paid for at the Contract unit price, per unit of measurement, for the following items:

(Delete Pay Item(s) from the list that are not included in the Schedule of Items, but do not change the alpha characters next to the pay items.)

Pay Item	Unit of Measurement

(a)	Curb Marking, Thermoplastic	Foot

(b)	Curb Marking, Paint	Foot

(c)	Non-Traversable Median Markings, Thermoplastic	Square Foot

(d)	Non-Traversable Median Markings Paint	Square Foot

Payment will be payment in full for furnishing and placing all Materials, and for furnishing all Equipment, labor, and Incidentals necessary to complete the Work as specified.