SP02830  (Special Provisions for the 2021 Book) 	(Bidding on or after: 12-01-20

Last updated: 08-19-20)

# SECTION 02830 - METAL HANDRAIL

(Follow all instructions and make all edits with “Track Changes” turned on. This Section is not published in the Oregon Standard. If there are no instructions [orange text] above a subsection, paragraph, sentence, or bullet, then include it in the project, unless the item(s) that are included in the subsection, paragraph, sentence, or bullet are not required on the Project and then they should be deleted. In general do not re-number or re-letter subsections when item(s) are deleted. Delete all orange text before preparing the final document. All other modifications to this Section will require ODOT Technical Resource and State Specifications Engineer approval.)

Section 02830, which is not a Standard Specification, is included in this Project by Special Provision.

## Description

02830.00  Scope - This Section includes the requirements for the steel in handrail for stairways and pedestrian facilities.

## Materials

02830.10  Shapes, Plates, and Bars - Shapes, plates, and bars shall conform to ASTM A36.

Punch anchor plate bolt holes at the locations shown before fabrication.

02830.20  Steel Pipe - Steel pipe shall conform to ASTM A500, seamless, Grade B.

02830.21  Steel Tube - Steel tube shall conform to ASTM A500, seamless, Grade B.

02830.22  Fasteners - Fasteners shall meet the requirements of Section 02560. Machine screws shall be SAE 18 8 stainless steel.

02830.30  Galvanizing - Hot-dip galvanize all handrail components according to AASHTO M 111 (ASTM A123) after shop fabrication.

02830.31  Repair of Hot-Dip Galvanizing - Repair damaged hot-dip galvanizing according to ASTM A780 and ASTM A123. Minimum zinc content for Method A2 is 94 percent on the dry film.

02830.40  Incidentals - Plates, caps, and miscellaneous pieces necessary to complete the rail shall be as shown.

02830.50  Acceptance - Acceptance of handrail Materials will be according to 00165.35 and this Section.