SP02831  (Special Provisions for the 2021 Book) 	(Bidding on or after: 12-01-20

Last updated: 08-19-20)

# SECTION 02831 - PEDESTRIAN FENCE

(Follow all instructions and make all edits with “Track Changes” turned on. This Section is not published in the Oregon Standard. If there are no instructions [orange text] above a subsection, paragraph, sentence, or bullet, then include it in the project, unless the item(s) that are included in the subsection, paragraph, sentence, or bullet are not required on the Project and then they should be deleted. In general do not re-number or re-letter subsections when item(s) are deleted. Delete all orange text before preparing the final document. All other modifications to this Section will require ODOT Technical Resource and State Specifications Engineer approval.)

Section 02831, which is not a Standard Specification, is included in this Project by Special Provision.

## Description

02831.00  Scope - This Section includes the requirements for the metals in pedestrian fence.

## Materials

02831.10  Aluminum Parts - Posts, post caps, post bases, rails, and spindles shall conform to 6061-T6 aluminum. Punch post base bolt holes at the locations shown before fabrication.

02831.20  Fasteners - Fasteners shall meet the following requirements:

Threaded rods – 	ASTM A193 Grade B7 Galvanized

1/2 inch dia. steel nuts – 	ASTM A194 Grade 8M Galvanized

1/2 inch dia. SAE steel flat washers – 	ASTM F436 Type 1 Galvanized

02831.40  Acceptance - Acceptance of pedestrian rail Materials will be according to 00165.35 and this Section.