SP00566  (Special Provisions for the 2021 Book) 	(Bidding on or after: 12-01-21

Last updated: 09-02-21)

# SECTION 00566 - CARBON FIBER REINFORCED POLYMER STRENGTHENING - NEAR SURFACE MOUNTED

(Follow all instructions and make all edits with “Track Changes” turned on. If there are no instructions [orange text] above a subsection, paragraph, sentence, or bullet, then include it in the project. Delete all orange text before preparing the final document. All other modifications to this Section will require ODOT Technical Resource and State Specifications Engineer approval.)

Comply with Section 00566 of the Standard Specifications modified as follows:

00566.11  Epoxy Resin - Replace this subsection, except for the subsection number and title, with the following:

Furnish epoxy resin from the QPL having a viscosity appropriate for the installation, as determined by the CFRP manufacturer. With the Engineer’s approval, epoxy resin recommended by the CFRP manufacturer may be used to complete the NSM-CFRP system.

00566.41  Saw-Cutting Grooves - Add the following sentence to the end of the paragraph that begins “Groove spacing may be adjusted…”

Maintain a minimum clear spacing greater than twice the depth of the groove and a minimum clear edge distance of four times the depth of the groove.

00566.80  Measurement - Add the following to the end of this subsection:

The estimated length of required CFRP bars is shown below.

(Obtain structure number and quantities from the Bridge Designer.)

Structure	Quantity

(Feet)

Bridge No. ________

Bridge No. ________