SP00756  (Special Provisions for the 2021 Book) 	(Bidding on or after: 09-01-21

Last updated: 05-26-21

This Section requires SP02001

and SP02050

Requires 02510 if epoxy coated

reinforcement is required)

# SECTION 00756 - PLAIN CONCRETE PAVEMENT

(Follow all instructions and make all edits with “Track Changes” turned on. If there are no instructions [orange text] above a subsection, paragraph, sentence, or bullet, then include it in the project. Delete all orange text before preparing the final document. All other modifications to this Section will require ODOT Technical Resource and State Specifications Engineer approval.)

Comply with Section 00756 of the Standard Specifications modified as follows:

00756.15(a)  Concrete Mixture - Replace this subsection, except for the subsection number and title, with the following:

Sample and test according to the MFTP.

For all plain concrete pavement, provide personnel according to 00756.30 to sample and test the mix for temperature, air content, slump, water-cementitious ratio, density and yield, from the first load of each placement, whenever there is a visible change in the slump of the concrete, and when a set of cylinders is obtained.

If the results of any test are outside of the Specification limits, stop the placement of the load. Correct the load or reject it and do not incorporate it into the Work. Test subsequent loads before any further concrete placement. Correct the subsequent loads if any of the tests are still outside the Specification limits. If the load cannot be corrected, reject it and do not incorporate it into the Work. Testing of subsequent loads may return to the specified frequency when the test results from two consecutive loads are shown to meet the Specification limits.

00756.95(a)  General - Replace the bullet that begins “The average of the IRI for both…” with the following bullet:

The IRI in each wheel path is 65.0 inches per mile or less.