SP02530  (Special Provisions for the 2021 Book) 	(Bidding on or after: 12-01-22

Last updated: 09-1-22)

# SECTION 02530 - STRUCTURAL STEEL

(Follow all instructions and make all edits with “Track Changes” turned on. If there are no instructions [orange text] above a subsection, paragraph, sentence, or bullet, then include it in the project. Delete all orange text before preparing the final document. All other modifications to this Section will require ODOT Technical Resource and State Specifications Engineer approval.)

Comply with Section 02530 of the Standard Specifications modified as follows:

02530.10  Structural Steel for Bridges - Replace this subsection, except for the subsection number and title, with the following:

Structural steel for Bridges shall conform to the following, as shown or specified:

AASHTO M 270, Grade 36 (ASTM A709, Grade 36)

AASHTO M 270, Grade 50 (ASTM A709, Grade 50)

AASHTO M 270, Grade 50W (ASTM A709, Grade 50W)

AASHTO M 270, Grade HPS 70 (ASTM A709 Grade HPS 70)

AASHTO M 270, Grade HPS 70W (ASTM A709 Grade HPS 70W)

Impact test requirements, for both non-fracture-critical tension components (T), and fracture-critical tension components (F), are to be according to Zone 2 requirements of AASHTO M 270 Tables 11 and 12, respectively.