SP02690  (Special Provisions for the 2021 Book) 	(Bidding on or after: 09-01-23

Last updated: 05-16-23)

# SECTION 02690 - PCC AGGREGATES

(Follow all instructions and make all edits with “Track Changes” turned on. If there are no instructions [orange text] above a subsection, paragraph, sentence, or bullet, then include it in the project. Delete all orange text before preparing the final document. All other modifications to this Section will require ODOT Technical Resource and State Specifications Engineer approval.)

Comply with Section 02690 of the Standard Specifications modified as follows:

02690.20(a)  Harmful Substances - In the paragraph that begins “Material passing No. 200 sieve…”, replace the words “T 11” with the words “T 27 / T 11”.

02690.20(e)  Grading and Separation by Sizes for Prestressed Concrete - Replace this subsection with the following subsection:

02690.20(e)  Grading and Separation by Sizes - Sampling shall be according to AASHTO R 90. Sieve analysis shall be according to AASHTO T 27 and AASHTO T 11. Provide aggregates meeting the gradation requirements of Table 02690-1 for structural concrete. Provide a CAgT to perform sampling and testing when required.

Table 02690-1

Gradation of Coarse Aggregates

Percent passing (by Weight)

02690.20(f)  Grading and Separation by Sizes for Other Concrete - Delete this subsection.

02690.30(b)  Harmful Substances - In the paragraph that begins “Material passing No. 200 sieve…”, replace the words “T 11” with the words “T 27 / T 11”.

02690.30(g)  Grading - In the paragraph that begins “Sampling shall be according to…”, replace the words “AASHTO T 2” with the words “AASHTO R 90”.