SP00333  (Special Provisions for the 2024 Book) 	(Bidding on or after: 12-01-23

Last updated: 05-19-23)

# SECTION 00333 - AGGREGATE DITCH LINING

(Follow all instructions and make all edits with “Track Changes” turned on. This Section is not published in the Oregon Standard. If there are no instructions [orange text] above a subsection, paragraph, sentence, or bullet, then include it in the project, unless the item(s) that are included in the subsection, paragraph, sentence, or bullet are not required on the Project and then they should be deleted. In general do not re-number or re-letter subsections when item(s) are deleted. Delete all orange text before preparing the final document. All other modifications to this Section will require ODOT Technical Resource and State Specifications Engineer approval.)

Section 00333, which is not a Standard Specification, is included in this Project by Special Provision.

## Description

00333.00  Scope - This Work consists of furnishing and placing aggregate ditch lining at locations shown or directed.

## Materials

00333.10  Aggregate Ditch Lining - Provide hard durable rock or gravel with a moisture binder of clay material that provides a tight, erosion-resistant surface meeting the following grading requirements:

Sieve Size Passing	Percentages (by Weight)

6"	100

4"	30 - 50

2"	20 - 30

No. 200	15 - 25

## Construction

00333.40  General - Place the aggregate material to the lines and grades established and as shown.

## Measurement

00333.80  Measurement - The quantities of aggregate ditch lining will be measured on the area basis of the actual surface area of the wetted perimeter of the lined ditch.

Ditch excavation will be measured according to 00330.80 and 00330.81.

## Payment

00333.90  Payment - The accepted quantities of aggregate ditch lining will be paid for at the Contract unit price, per square yard, for the item "Aggregate Ditch Lining".

Payment will be payment in full for furnishing all Materials, and for furnishing all Equipment, labor, and Incidentals necessary to complete the Work as specified.

Ditch excavation will be paid for according to 00330.90, 00330.91, and 00330.93.