SP00744  (Special Provisions for the 2024 Book) 	(Bidding on or after: 12-01-23

Last updated: 05-23-23

This Section requires SP00730

This Section requires SP00738 when

Safety Edge is shown in the typical

sections of the plans.)

# SECTION 00744 - ASPHALT CONCRETE PAVEMENT

(Follow all instructions and make all edits with “Track Changes” turned on. If there are no instructions [orange text] above a subsection, paragraph, sentence, or bullet, then include it in the project. Delete all orange text before preparing the final document. All other modifications to this Section will require ODOT Technical Resource and State Specifications Engineer approval.)

Comply with Section 00744 of the Standard Specifications modified as follows:

(Fill in the blank with the required grade of asphalt used on the project.)

00744.11(a)  Asphalt Cement - Add the following to the end of this subsection:

Provide _______ grade asphalt cement for this Project.

(Use the following subsection .16 on projects that are bid and awarded by ODOT. The following subsection is not intended for use on projects that are not bid and awarded by ODOT.)

00744.16  Sampling and Testing - Replace this subsection, except for the subsection number and title, with the following:

For each 1,000 Tons of placement, have a CAT I perform a minimum of one of each of the following test methods as modified in the MFTP:

Asphalt Content - AASHTO T 308 with ODOT TM 323 determined Calibration Factor

Gradation - AASHTO T 30

Mix Moisture - AASHTO T 329

Maximum Specific Gravity - AASHTO T 209

Field Compacted Gyratory Specimens - ODOT TM 326

When less than 1,000 Tons of mix is placed in a Day, perform a minimum of one series of tests per Day. Provide test results to the Engineer by the middle of the following work shift.  The Engineer may waive the requirement for any of AASHTO T 308, AASHTO T 30, AASHTO T 329, and ODOT TM 326 on a daily basis. The Engineer may waive the requirement for AASHTO T 209 when less than 500 Tons of ACP is placed in a single work shift.

Provide samples or split samples to the Engineer when requested.

(Use the following subsection .17 on projects that are bid and awarded by ODOT. The following subsection is not intended for use on projects that are not bid and awarded by ODOT.)

00744.17  Acceptance - Replace this subsection, except for the subsection number and title, with the following:

If the test result for each mix gradation constituent, asphalt content, and density measurement is within the specification limits, the material will be accepted. If the asphalt content, one or more gradation constituents, or the density measurement are not within the specification limits, the material that is not within the specification limits will be accepted according to 00150.25.

(Use the following subsection .41 on projects that are bid and awarded by ODOT. The following subsection is not intended for use on projects that are not bid and awarded by ODOT.)

00744.41  Mixing Temperature - Replace the table with the following:

Temperature, °F

Type	Maximum	Minimum Behind

at Mixer	Paver

HMAC	350	240

WMAC	350	215

(Use the following subsection .49 on projects that are bid and awarded by ODOT. The following subsection is not intended for use on projects that are not bid and awarded by ODOT.)

00744.49  Compaction - Replace the paragraph that begins "Determine compliance with…" with the following paragraph:

Determine compliance with density Specifications by random testing of the compacted surface with calibrated nuclear gauges. Determine the density by averaging QC tests performed by a CDT with the nuclear gauge operated in the backscatter mode according to AASHTO T 355 at one random location for each 100 Tons of asphalt concrete placed, but take no less than 10 tests each shift. Do not locate the center of a density test less than 1 foot from the Panel edge. Calculate MAMD according to ODOT TM 305. The Engineer may waive compaction testing requirements when less than 500 Tons of ACP is placed in a single work shift.

(Use the following lead-in paragraph and one of the following two options when traffic restrictions are required. Obtain information from the pavement designer. Delete the option that does not apply.)

Add the following subsection:

[ Option 1 - Use this .51 when paving through the top base course is required. ]

00744.51  Opening Sections to Traffic - Schedule work so that, during the same shift, the surfaces being paved are paved full width and length through the top Base Course before opening to traffic. Traffic will be allowed on the top Base Course up to ____ Calendar Days.

Before beginning wearing Course paving operations, make repairs to the existing surface as directed. Payment for the repairs will be made according to 00195.20.

[ Option 2 - Use this .51 when paving through the wearing course is required. ]

00744.51  Opening Sections to Traffic - Schedule work so that, during the same shift, the surfaces being paved are paved full width and length through the wearing Course before opening to traffic.