SP02320  (Special Provisions for the 2024 Book) 	(Bidding on or after: 05-01-25

Last updated: 01-24-25)

# SECTION 02320 - GEOSYNTHETICS

(Follow all instructions and make all edits with “Track Changes” turned on. If there are no instructions [purple text] above a subsection, paragraph, sentence, or bullet, then include it in the Project. Delete all purple text before preparing the final document. All other modifications to this Section will require ODOT Technical Resource and State Specifications Engineer approval.)

Comply with Section 02320 of the Standard Specifications modified as follows:

02320.20  Geotextile Property Values – Replace Table 02320-3 with the following table:

Table 02320-3  Geotextile Property Values for Sediment Fence 1

| Geotextile Property | ASTM Test Method | Unit | Geotextile Property Requirements Woven and Nonwoven |
| --- | --- | --- | --- |
| Grab Tensile Strength (minimum) Machine and Cross Machine Directions | D 4632 | lb | 120 100 |
| Apparent Opening Size (AOS) (maximum) U.S. Standard Sieve | D 4751 | — | 30 |
| Permittivity (minimum) | D 4491 | sec-1 | 0.05 |
| Ultraviolet Stability Retained Strength (minimum) | D 4355 (at 500 hours) | % | 70 |

1	All geotextile properties are Minimum Average Roll Values (MARV).  The test results for any sampled roll in a lot shall meet or exceed the values shown in the table.