SP00735  (Special Provisions for the 2024 Book) 	(Bidding on or after: 06-01-25

Last updated: 03-03-25

This Section require SP00705 when

emulsified asphalt fog coat is required.

Requires SP00710 or SP00715 when

chip seal is required.)

# SECTION 00735 - EMULSIFIED ASPHALT CONCRETE PAVEMENT

(Follow all instructions and make all edits with “Track Changes” turned on. If there are no instructions [purple text] above a subsection, paragraph, sentence, or bullet, then include it in the project. Delete all purple text before preparing the final document. All other modifications to this Section will require ODOT Technical Resource and State Specifications Engineer approval.)

Comply with Section 00735 of the Standard Specifications modified as follows:

00735.40  Season and Weather Limitations - Replace the title of this subsection with “Weather Limitations”.

Replace the paragraph that begins "Place EAC from May 1 to August 31…" with the following paragraph:

Place EAC from May 1 to August 31, inclusive, when the Pavement temperature is 60 °F or above. Limitations for EAC will not supersede limitations for Emulsified Asphalt chip seals on the Project.

00735.42  Preparation of Underlying Surfaces – Add the following paragraph to the end of this subsection:

Remove existing pavement markers, recessed markers, and pavement legends before paving. Remove pavement lines, bars, and pavement legends as shown or directed and according to 00225.45.

(Use the following subsection .45(b) on projects that allow alternate methods of depositing EAC on the road. Obtain the methods from the Designer.)

00735.45(b)  Depositing - Add the following to the end of this subsection:

The following alternate methods of depositing EAC may be used: