SP02001  (Special Provisions for the 2024 Book) 	(Bidding on or after: 07-01-25

Last updated: 04-01-25

Requires SP02690 when IC, LWFA

or lightweight coarse aggregate is required.)

# SECTION 02001 - CONCRETE

(Follow all instructions and make all edits with “Track Changes” turned on. If there are no instructions [purple text] above a subsection, paragraph, sentence, or bullet, then include it in the Project. Delete all purple text before preparing the final document. All other modifications to this Section will require ODOT Technical Resource and State Specifications Engineer approval.)

Comply with Section 02001 of the Standard Specifications modified as follows:

02001.15(b)(2)(d)  Permeability Tests - Replace this subsection, except for the subsection number and title, with the following:

For alternate HPC mix designs, select from the following options:

Make at least three specimens from the trial batch for permeability testing. Prepare, cure, dry and test according to AASHTO T 277. Report permeability in coulombs at 90 Days.

Make at least two specimens from the trial batch for resistivity testing. Prepare, cure and test according to AASHTO T358 using the sealed conditioning method. Report resistivity in kΩꞏcm at 56 Days.

02001.20(e)  Durability - Replace the paragraph that begins "1 Only required for alternate HPC designs. See …" with the following paragraph:

1 Only required for alternate HPC designs. See 02001.30(b)(2). A minimum resistivity of 37.0 kΩꞏcm at 56 Days for 4x8 inch cylinders and 29 kΩꞏcm at 56 Days for 6x12 inch cylinders will be accepted as equal when tested according to AASHTO T358 using the sealed conditioning method.

(Use the following lead-in paragraph and subsection .20(f) when IC is specified to mitigate shrinkage in Bridge decks. Contact ODOT Structure Services prior to selecting internal curing)

Add the following subsection:

02001.20(f)  Internal Curing - For HPC(IC) concrete, internally cure the mixture according to the following:

Substitute 350 lbs (SSD) LWFA for standard Fine Aggregate.

(Use the following lead-in paragraph and subsection .20(g) when lightweight concrete is required. Contact the Statewide Structural Materials Engineer who will provide densities to be used to fill in the blanks.)

Add the following subsection:

02001.20(g)  Unit Weight - Provide high performance lightweight concrete with a maximum plastic density of _____ pounds per cubic foot at time of placement and a maximum calculated approximate equilibrium density of _____ pounds per cubic foot.

02001.30(a)  Portland Cement - Replace this subsection, except for the subsection number and title, with the following:

For structural or paving concrete applications use cement according to 02010.10 or 02010.20, excluding Type III. Use Type III cement for precast prestressed concrete.

02001.30(b)(2)  HPC Cementitious Composition - Replace this subsection, except for the subsection number and title, with the following:

Cement with SCM proportioned according to 02001.30(b)(1) and with trial batches performed to demonstrate that the proposed alternate mix design provides a maximum of 1,000 coulombs at 90 Days when tested according to AASHTO T 277 or a minimum resistivity of 37.0 kΩꞏcm at 56 Days for 4x8 inch cylinders and 29 kΩꞏcm at 56 Days for 6x12 inch cylinders will be accepted as equal when tested according to AASHTO T358 using the sealed conditioning method.

02001.40(b)  Adjusting Concrete Proportions - Replace the bullet that begins "Large admixture dosage changes…" with the following bullet:

Large admixture dosage changes, excluding adjustments for air entraining agents and Type A or D water reducers (± 25 oz/cubic yard).