SP02910  (Special Provisions for the 2024 Book) 	(Bidding on or after: 07-01-25

Last updated: 04-01-25

Required when sign panels

require anti-graffiti coating.)

# SECTION 02910 - SIGN MATERIALS

(Follow all instructions and make all edits with “Track Changes” turned on. If there are no instructions [purple text] above a subsection, paragraph, sentence, or bullet, then include it in the Project. Delete all purple text before preparing the final document. All other modifications to this Section will require ODOT Technical Resource and State Specifications Engineer approval.)

Comply with Section 02910 of the Standard Specifications modified as follows:

Add the following subsection:

02910.23  Digital Printing -

(a)  Digitally Printed Ink Systems – Provide digitally printed ink systems from the QPL that meet the following requirements:

Produce traffic signs using components, and processes that comply with the retroreflective sheeting manufacturer’s recommendations.

Meet and comply with daytime and nighttime chromaticity (color standards) as recognized in ASTM D4956 Standard Specification for Retroreflective Sheeting for Traffic Control.

Meet 70% for type XI standards of the initial retroreflectivity specifications of each respective reflective film color as found in ASTM D4956.

(b)  Retroreflective Sheeting – Furnish retroreflective sheeting that:

Consists of white or colored sheeting having a smooth outer surface and that has the property of a retroreflector over its entire surface.

Conform to all requirements of the current version of ASTM D4956. Designate the retroreflective sheeting as type XI ASTM D4956 classification.

Has a Class 1 pressure-sensitive adhesive, as defined by ASTM D4956, protected by an easily removable liner. Fabricate finished traffic signs and traffic sign faces using retroreflective sheeting of Type XI ASTM D4956 classification.

(c)  Protective Overlay Film – Fabricate permanent traffic signs printed with digital ink systems with a full sign protective overlay film designed to provide a smooth surface needed for retroreflectivity, and to protect the sign from fading and UV degradation. Comply with the retroreflective sheeting manufacturer’s recommendations for the overlaminate to ensure proper adhesion and transparency. Meet the reflective film durability as identified in the warranty requirements.

02910.33  Permanent Legends – Replace this subsection, except for the subsection number and title, with the following:

(a)  General – Permanent legends consist of white retroreflective screened, red retroreflective screened, black screened or cut-out white retroreflective sheeting. Meet the design of the FHWA Standard Rounded Capital Letter Alphabets for the letters and numerals of all permanent legends.

(b)  Retroreflective White Screened Legend – Use transparent paste materials for the reverse screening of retroreflective white legends and for the screening of retroreflective red legends conforming to the recommendations of the manufacturer of the reflective sheeting.

(c)  Retroreflective Cut-out Legend – Use Material for retroreflective cut-out legend conforming to the requirements of 02910.20.

(d)  Nonreflective Black Screened Legend – Furnish Material for nonreflective black screened legends that is compatible with the sign sheeting, as recommended by the sign sheeting manufacturer.

(e)  Nonreflective Black Cut-out Legend – Use Material for nonreflective cut-out legend conforming to 02910.21.

(f)  Digitally Printed Sign – Use processes and Materials for digitally printed signs conforming to the requirements of 02910.23.

(Use subsection .70 when sign panels require anti-graffiti coating.)

Add the following subsection:

02910.70  Anti-Graffiti Coating for Signs:

(a)  General - Use anti-graffiti coating from the QPL. Apply anti-graffiti coating over both the background and legend sheeting, per the manufacturer’s recommendation.

(b)  Acceptance - Furnish a quality compliance certificate according to 00165.35, certifying that the anti-graffiti coating used is an acceptable product on the QPL.