SP00360  (Special Provisions for the 2024 Book) 	(Bidding on or after: 09-01-25

Last updated: 05-29-25)

# SECTION 00360 - DRAINAGE BLANKETS

(Follow all instructions and make all edits with “Track Changes” turned on. This Section is not published in the Oregon Standard. If there are no instructions [purple text] above a subsection, paragraph, sentence, or bullet, then include it in the project, unless the item(s) that are included in the subsection, paragraph, sentence, or bullet are not required on the Project and then they should be deleted. In general do not re-number or re-letter subsections when item(s) are deleted. Delete all purple text before preparing the final document. All other modifications to this Section will require ODOT Technical Resource and State Specifications Engineer approval.)

Section 00360, which is not a Standard Specification, is included in this Project by Special Provision.

## Description

00360.00  Scope - This Work consists of furnishing and placing drainage blanket material to the lines, grades and dimensions shown, or as directed.

## Materials

(Use the following subsection .10 when sand drainage blanket material is required.)

00360.10  Sand Drainage Blanket - Furnish sand drainage blanket Material meeting the following gradation limits determined by AASHTO T 27 and AASHTO T 11:

Sieve Size	Percent Passing

No. 10	95 - 100

No. 40	50 - 100

No. 60	20 - 40

No. 200	0.0 - 5.0

(Use the following subsection .11 when granular drainage blanket material is required.)

00360.11  Granular Drainage Blanket - Furnish granular drainage blanket Material that is clean, free draining, durable crushed or uncrushed Rock, meeting the following gradation limits determined by AASHTO T 27:

Sieve Size	Percent Passing

6"	100

4"	90 - 100

1/2"	60 - 80

No. 10	0 - 10

No. 100	0 - 5

Granular drainage blanket material will be accepted without testing if the Engineer visually determines the material meets the above requirements.

00360.15  Quality Control - Provide quality control according to Section 00165.

## Equipment

00360.20  General - Use Equipment capable of hauling, spreading and compacting the material to specified density without segregation.

If drainage blanket material is used to drain areas described in 00360.41, hauling with end dump trucks and spreading with bulldozers and other appropriate Equipment will be allowed.

## Labor

00360.30  Quality Control Personnel - Provide technicians having CEBT, CAgT, and CDT technical certifications.

## Construction

00360.40  Planned Locations - On prepared excavations or embankments constructed as shown on the Plans or as directed, place the drainage blanket as follows:

Spread and compact to required depth with no layer exceeding 3 feet.

If a subsurface drain system is installed immediately under or adjacent to the drainage blanket, place the drainage blanket directly against the subsurface drain system.

Prevent contamination of drainage blanket material.

00360.41  Other Locations - When used to drain an unstable or wet area, excavate or trench the existing low areas as directed for positive drainage before placement of drainage blanket material.

00360.42  Compaction and Density Requirements - Compact the drainage blanket according to 00330.43.

(Delete the language in purple parentheses that does not apply and delete all purple parentheses.)

## Measurement

00360.80  Measurement - The (quantity)(quantities) of (sand) (and) (granular) drainage blanket Material will be measured on the volume basis in place and will be limited to the Neat Lines, grades, and dimensions shown or directed, or on the weight basis.

## Payment

(Delete the language in purple parentheses that does not apply and delete all purple parentheses. Delete the "(s)" or parentheses from the word "item(s)" as appropriate.)

00360.90  Payment - The accepted (quantity)(quantities) of (sand) (and) (granular) drainage blankets will be paid for at the Contract unit price, per unit of measurement, for the following item(s):

(Delete pay item(s) from the list that are not included in the Schedule of Items, but do not change the alpha characters next to the pay items.)

Pay Item	Unit of Measurement

(a)	Sand Drainage Blanket	Cubic Yard or Ton

(b)	Granular Drainage Blanket	Cubic Yard or Ton

Payment will be payment in full for furnishing and placing all Materials, and for furnishing all Equipment, labor, and Incidentals necessary to complete the Work as specified.