SP02320  (Special Provisions for the 2024 Book) 	(Bidding on or after: 09-01-25

Last updated: 06-02-25)

# SECTION 02320 - GEOSYNTHETICS

(Follow all instructions and make all edits with “Track Changes” turned on. If there are no instructions [purple text] above a subsection, paragraph, sentence, or bullet, then include it in the Project. Delete all purple text before preparing the final document. All other modifications to this Section will require ODOT Technical Resource and State Specifications Engineer approval.)

Comply with Section 02320 of the Standard Specifications modified as follows:

(Use the following subsection .10(a)(3) when geomembranes are required.)

Add the following subsection:

02320.10(a)(3)  Geomembranes - Furnish geomembranes which meet or exceed the properties specified in 02320.30 for the applicable resin type and thickness.

(Use the following subsection .10(c)(3) when geomembranes are required.)

Add the following subsection:

02320.10(c)(3)  Geomembranes - Include the following:

Average roll values for each of the specified properties from the same production run as the delivered material.

Production run number, production plant name, and location.

Manufacturer's name and address.

Full product name and information.

Identify the resin type and location for use referencing the Plans drawing number.

(Use the following subsection .10(d)(4) when geomembranes are required.)

Add the following subsection:

02320.10(d)(4)  Geomembrane Testing - Perform the specified tests to determine the geomembrane properties for the type and thickness of membrane.

(Use the following subsection .11 when geomembranes are required.)

02320.11  Seam Testing and Acceptance - Replace the title of this subsection with “Geotextile Seam Testing and Acceptance”

(Use the following subsection .12 when geomembranes are required.)

Add the following subsection:

02320.12  Geomembrane Seam Testing and Acceptance:

(a)  Geomembrane Factory Seams - Factory seams are not allowed in HDPE and LLDPE geomembrane; provide HDPE and LLDPE geomembrane as continuous sheets in rolls. Provide PVC geomembrane with factory seams in the panels to reduce field seaming and testing.

(b)  Geomembrane Field Seams - Perform geomembrane field seam testing according to 00350.43.

(Use the following subsection .20 when sediment fence is required.)

02320.20  Geotextile Property Values – Replace Table 02320-3 with the following table:

Table 02320-3  Geotextile Property Values for Sediment Fence 1

| Geotextile Property | ASTM Test Method | Unit | Geotextile Property Requirements Woven and Nonwoven |
| --- | --- | --- | --- |
| Grab Tensile Strength (minimum) Machine and Cross Machine Directions | D 4632 | lb | 120 100 |
| Apparent Opening Size (AOS) (maximum) U.S. Standard Sieve | D 4751 | — | 30 |
| Permittivity (minimum) | D 4491 | sec-1 | 0.05 |
| Ultraviolet Stability Retained Strength (minimum) | D 4355 (at 500 hours) | % | 70 |

1	All geotextile properties are Minimum Average Roll Values (MARV).  The test results for any sampled roll in a lot shall meet or exceed the values shown in the table.

(Use the following subsection .30 and tables when geomembranes are required.)

Add the following subsection:

02320.30  Geomembrane Property Values:

Table 02320-7a  Property Values for High Density Polyethylene (HDPE) Geomembrane – Textured

|  | ASTM Test Method |  |  | Test | Value |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Properties |  | 30 mils | 40 mils |  |  | 50 mils | 60 mils |
| Thickness mils (min. ave.) - mils | D5994 | nom. -5% | nom. -5% |  |  | nom. -5% | nom. -5% |
| Formulated Density (min. ave.) - g/cc | D1505/D792 | 0.94 | 0.94 |  |  | 0.94 | 0.94 |
| Tensile Properties (min. ave.) | D 6693 |  |  |  |  |  |  |
| • yield strength - lb/in. | Type IV | 63 | 84 |  |  | 105 | 126 |
| • break strength - lb/in. |  | 45 | 60 |  |  | 75 | 90 |
| • yield elongation - % |  | 12 | 12 |  |  | 12 | 12 |
| • break elongation - % |  | 100 | 100 |  |  | 100 | 100 |
| Tear Resistance (min. ave.) - lb | D1004 | 21 | 28 |  |  | 35 | 42 |
| Puncture Resistance (min. ave.) - lb | D4833 | 45 | 60 |  |  | 75 | 90 |
| Stress Crack Resistance - hr. | D5397 (App) | 500 | 500 |  |  | 500 | 500 |
| Carbon Black Content (range) - % | D4218 | 2.0 - 3.0 | 2.0 - 3.0 |  |  | 2.0 - 3.0 | 2.0 - 3.0 |

Table 02320-7b  Property Values for Linear Low Density Polyethylene (LLDPE) Geomembrane – Textured

|  | ASTM Test Method |  |  | Test | Value |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Properties |  | 30 mils | 40 mils |  |  | 50 mils | 60 mils |
| Thickness mils (min. ave.) - mils | D5994 | nom. -5% | nom. -5% |  |  | nom. -5% | nom. -5% |
| Formulated Density (max) - g/cc | D1505/D792 | 0.94 | 0.94 |  |  | 0.94 | 0.94 |
| Tensile Properties (min. ave.) | D 6693 |  |  |  |  |  |  |
| • break strength - lb/in. | Type IV | 30 | 45 |  |  | 60 | 75 |
| • break elongation - % |  | 250 | 250 |  |  | 250 | 250 |
| 2% Modulus - lb/in - (max) | D5323 | 1200 | 1800 |  |  | 2400 | 3000 |
| Tear Resistance (min. ave.) - lb | D1004 | 11 | 16 |  |  | 22 | 27 |
| Puncture Resistance (min. ave.) - lb | D 4833 | 22 | 33 |  |  | 44 | 55 |
| Axi-Symmetric Break resistance Strain (min) - % | D5617 | 30 | 30 |  |  | 30 | 30 |
| Carbon Black Content (range) - % | D4218 | 2.0 - 3.0 | 2.0 - 3.0 |  |  | 2.0 - 3.0 | 2.0 - 3.0 |

Table 02320-7c Property Values for Non-Reinforced Polyvinyl Chloride (PVC) Geomembrane Used in Buried Applications

|  | ASTM Test Method |  |  | Test | Value |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Properties |  | 30 mils | 40 mils |  |  | 50 mils | 60 mils |
| Thickness mils (min. ave.) - mils | D5994 | nom. -5% | nom. -5% |  |  | nom. -5% | nom. -5% |
| Tensile Properties (min.) | D982 |  |  |  |  |  |  |
| • break strength - lb/in. |  | 73 | 97 |  |  | 116 | 137 |
| • break elongation - % |  | 380 | 430 |  |  | 430 | 450 |
| • Modulus at 100% - lb/in |  | 30 | 40 |  |  | 50 | 60 |
| Tear Strength (min.) - lb | D1004 | 8 | 10 |  |  | 13 | 15 |
| Dimensional Stability (max change) - % | D1204 | 3 | 3 |  |  | 3 | 3 |
| Low Temperature Impact Pass ( ˚F) | D1790 | -20 | -20 |  |  | -20 | -20 |
| Specific Gravity (min) | D790 | 1.2 | 1.2 |  |  | 1.2 | 1.2 |
| Water Extraction (max loss) - % | D1239 | 0.15 | 0.20 |  |  | 0.20 | 0.20 |
| Volatile Loss (max loss) - % | D1203 | 0.70 | 0.50 |  |  | 0.50 | 0.50 |
| Soil Burial (max change) - % | G160 |  |  |  |  |  |  |
| Break Strength |  | 5 | 5 |  |  | 5 | 5 |
| Elongation |  | 20 | 20 |  |  | 20 | 20 |
| Modulus at 100% |  | 20 | 20 |  |  | 20 | 20 |
| Hydrostatic Resistance (min.) - psi | D751 | 100 | 120 |  |  | 150 | 180 |
| Minimum Average Molecular Weight | D8133 | 400 | 400 |  |  | 400 | 400 |