SP02630  (Special Provisions for the 2024 Book) 	(Bidding on or after: 09-01-25

Last updated: 05-29-25)

# SECTION 02630 – BASE AGGREGATE

(Follow all instructions and make all edits with “Track Changes” turned on. If there are no instructions [purple text] above a subsection, paragraph, sentence, or bullet, then include it in the Project. Delete all purple text before preparing the final document. All other modifications to this Section will require ODOT Technical Resource and State Specifications Engineer approval.)

Comply with Section 02630 of the Standard Specifications modified as follows:

02630.11(a)  Grading – Replace this subsection, except for the subsection number and title, with the following:

Provide open-graded Aggregate meeting the following grading requirements:

Table 02630-2

Aggregate Gradation for Open-Graded Aggregate

Percent Passing

Sieve Size	(by Weight)

1"	100

3/4"	80 - 98

1/2"	60 - 85

3/8"	30 - 45

No. 100	0 - 6 (Dry Sieve)

02630.11(b)  Fracture of Rounded Rock – Replace this subsection, except for the subsection number and title, with the following:

Determine fracture of rounded Rock according to AASHTO T 335. Provide Open-graded Aggregate meeting the following fracture requirements:

Percentage of Fracture (by Weight)

Material Retained on 3/4", 1/2", and 1/4" Sieves (two fractured faces) ........... 90