SP00440  (Special Provisions for the 2024 Book) 	(Bidding on or after: 04-01-26

Last updated: 12-30-25)

# SECTION 00440 - COMMERCIAL GRADE CONCRETE

(Follow all instructions and make all edits with “Track Changes” turned on. If there are no instructions [purple text] above a subsection, paragraph, sentence, or bullet, then include it in the project. Delete all purple text before preparing the final document. All other modifications to this Section will require ODOT Technical Resource and State Specifications Engineer approval.)

Comply with Section 00440 of the Standard Specifications modified as follows:

00440.40(e)  Curing - Replace this subsection, except for the subsection number and title, with the following:

Cure CGC for a minimum of 7 Calendar Days by one of the following methods:

Cover with wet burlap, canvas, Sand, or other acceptable Material, and keep moist.

Apply curing compounds at a rate of not less than 1 gallon per 150 square feet. Do not use on surfaces that come into contact with adjacent pours and avoid overspray on exposed reinforcement. Use curing compounds according to the following:

Table 00440-1

| Section | Item | Type 1 or 1-D (Clear) | Type 2 (White-Pigmented) |
| --- | --- | --- | --- |
| 00480 | Drainage Curbs | * | * |
| 00599 | Slope Paving Curbs and Berm Paving | Yes | No |
| 00759 | Walks, Curb Ramps, Driveways, Surfacings, Curbs, and Islands | * | * |

*Use Type 2 except when the Engineer requires Type 1 or 1-D