SP00530  (Special Provisions for the 2024 Book) 	(Bidding on or after: 01-01-26

Last updated: 09-24-25

Requires SP02510. Requires

SP02513 when using Stainless Steel.)

# SECTION 00530 - STEEL REINFORCEMENT FOR CONCRETE

(Follow all instructions and make all edits with “Track Changes” turned on. If there are no instructions [purple text] above a subsection, paragraph, sentence, or bullet, then include it in the Project. Delete all purple text before preparing the final document. All other modifications to this Section will require ODOT Technical Resource and State Specifications Engineer approval.)

Comply with Section 00530 of the Standard Specifications modified as follows:

00530.10  Materials - Replace this subsection, except for the subsection number and title, with the following:

Concrete Inserts	02513.35

Deformed Bar Reinforcement 	02510.10

Deformed Bar Reinforcement (Stainless Steel)	02513.10

Dowels	02510.50

Dowels (Stainless Steel)	02513.50

Epoxy Coated Reinforcement	02510.11

Galvanized Coating	02510.30

Headed Bar Reinforcement	02510.25

Mechanical Splices	02510.20

Mechanical Splices (Stainless Steel)	02513.20

Ties and Supports	02510.60

Ties and Supports (Stainless Steel)	02513.60

Welded Wire Reinforcement	02510.40

00530.41(a)  Fabric - Replace this subsection with the following subsection:

00530.41(a)  Welded Wire Reinforcement - If welded wire reinforcement is shipped in rolls, straighten it into flat sheets before placing.

00530.41(b)  Ties and Supports – Replace the bullet that begins “When stainless steel rebar is specified…” with the following bullet:

When stainless steel reinforcing is specified, use stainless steel ties and supports meeting the requirements of 02513.60.

Delete the bullet that begins “Tie stainless steel reinforcement …”.

Delete the bullet that begins “Support stainless steel reinforcement…”.

Replace the bullet that begins "Do not allow direct contact between stainless …" with the following bullet:

Do not allow stainless steel reinforcement to directly contact ASTM A1035 CS reinforcement. Do not allow stainless steel reinforcement or ASTM A1035 CS reinforcement in direct contact with other reinforcement with a different type of metal. When stainless steel or ASTM A1035 CS reinforcing or dowels are located near other reinforcing with a different type of metal, use nylon or polyethylene spacers to maintain a minimum 1 inch clearance between the two metals and bind them with nylon cable ties. Where insufficient space exists to maintain this minimum, either bar may be sleeved with a continuous polyethylene or nylon tube extending at least 1 inch in each direction past the point of closest contact between the two dissimilar bars.

Add the following bullets to the end of the bullet list:

When ASTM A1035 CS reinforcing is specified, use epoxy coated ties and supports meeting the requirements of 02510.60(a).

00530.43  Splicing Welded Wire Fabric – Replace this subsection with the following subsection:

00530.43  Splicing Welded Wire Reinforcement - Overlap sheets of welded wire reinforcement as shown or provide edge and end laps not less than one mesh in width. Securely fasten sheets at the ends and edges according to 00530.41.

(Use the following subsection .80(a) when reinforcement is paid for on the lump sum basis. Remove tables that are not applicable to the Project. Add additional rows as necessary. Obtain information from the Bridge Designer. For ASTM A1035, include the chromium content letters (CS, CM, or CL).)

00530.80(a)  Lump Sum - Add the following to the end of this subsection:

The estimated quantity for uncoated reinforcement in pounds is:

| Structure Number | Grade 60 | Grade 80 | Grade 100 ASTM A615 | Grade 100 ASTM A706 | Grade 100 ASTM A1035 (____) |
| --- | --- | --- | --- | --- | --- |
| 1234 | 0 | 0 | 100 | 0 | 1000 |

The estimated quantity for coated reinforcement in pounds is:

| Structure Number | Grade 60 | Grade 80 | Grade 100 ASTM A615 | Grade 100 ASTM A706 | Grade 100 ASTM A1035 (____) |
| --- | --- | --- | --- | --- | --- |
| 1234 | 0 | 0 | 100 | 0 | 1000 |

The estimated quantity for stainless steel in pounds is:

| Structure Number | Grade 60 | Grade 75 |
| --- | --- | --- |

The estimated quantity for welded wire reinforcement in pounds is:

| Structure Number | Grade____ |
| --- | --- |

00530.90  Payment - Replace this subsection, except for the subsection number and title, with the following:

The accepted quantities of reinforcement will be paid for at the Contract unit price, per unit of measurement, for the following items:

Pay Item 	Unit of Measurement

(a)  Reinforcement, Grade _____ 		Lump Sum or Pound

(b)  Reinforcement, ASTM A1035 _____		Lump Sum or Pound	(c)  Coated Reinforcement, Grade ____ 		Lump Sum or Pound

(d)  Coated Reinforcement, ASTM A1035 _____		Lump Sum or Pound

(e)  Stainless Steel Reinforcement, Grade ____,		Lump Sum or Pound

(f)  Welded Wire Reinforcement, Grade ____		Lump Sum or Pound

In items (a), (c), (e), and (f) the grade of reinforcement will be inserted in the blank.

In items (b) and (d) the ASTM chromium content, “CS”, “CM”, or “CL” will be inserted in the blank.

Item (a) and (b) include fabricating and placing uncoated reinforcement as specified.

Item (c) and (d) include placing epoxy coated reinforcement as specified.

Item (e) includes fabricating and placing stainless steel reinforcement as specified.

Item (f) includes fabricating and placing welded wire reinforcement as specified.

Payment for reinforcement will be made when the reinforcement is incorporated into the concrete.

Payment will be payment in full for furnishing and placing all Materials, and for furnishing all Equipment, labor, and Incidentals necessary to complete the Work as specified.

No separate or additional payment will be made for clips, wire, separators, wire chairs, or other Material used in fastening the reinforcement in place.