SP02510  (Special Provisions for the 2024 Book) 	(Bidding on or after: 04-01-26

Last updated: 12-29-25)

# SECTION 02510 - REINFORCEMENT

(Follow all instructions and make all edits with “Track Changes” turned on. If there are no instructions [purple text] above a subsection, paragraph, sentence, or bullet, then include it in the Project. Delete all purple text before preparing the final document. All other modifications to this Section will require ODOT Technical Resource and State Specifications Engineer approval.)

Comply with Section 02510 of the Standard Specifications modified as follows:

02510.11(c)  Coated Reinforcement Ties and Supports - Delete this subsection.

02510.11(d)  Epoxy Coating Repair - Delete this subsection.

02510.20  Mechanical Splices - Replace this subsection, except for the subsection number and title, with the following:

Furnish mechanical splices from the QPL. Where bars of different sizes or strengths are connected, the strength of the smaller or weaker bar governs. Measure the total slip displacement after loading in tension to 30.0 ksi and relaxing to 3.0 ksi. The maximum allowed displacement for bars up to No. 14 is 0.01 inches. and is 0.03 inches for No. 18 bar.

Type 1 Mechanical Splices - Furnish Type 1 Mechanical Splices that develop at least 125 percent of the specified minimum yield strength of the reinforcing bars. Type 1 Mechanical Splices are not allowed for column bars.

Type 2 Mechanical Splices - Furnish Type 2 Mechanical Splices that develop at least 125 percent of the specified minimum yield strength of the reinforcing bars and 100 percent of the specified tensile strength of the reinforcing bars.

02510.30(d)  Ties and Support - Delete this subsection.

02510.60  Wire Reinforcement - Replace this subsection with the following subsection:

02510.60  Ties and Supports - Provide tie wire and supports according to CRSI Manual of Standard Practice.

(a)  Coated Reinforcement Ties and Supports – Provide nonmetallic coated ties and supports for coated reinforcement, including ties for coated-to-uncoated reinforcement connections.

(b)  Uncoated Reinforcement Ties and Supports - Tie all mats of galvanized steel bars with galvanized ties. Provide precast concrete blocks with galvanized ties that support galvanized reinforcement.