SP01013  (Special Provisions for the 2024 Book) 	(Bidding on or after: 07-01-26

Last updated: 04-02-26

Requires SP00842 and SP02640)

# SECTION 01013 - STORMWATER CONTROL, WATER QUALITY BIOSLOPE

(Follow all instructions and make all edits with “Track Changes” turned on. This Section is not published in the Oregon Standard. If there are no instructions [purple text] above a subsection, paragraph, sentence, or bullet, then include it in the Project, unless the item(s) that are included in the subsection, paragraph, sentence, or bullet are not required on the Project and then they should be deleted. In general do not re-number or re-letter subsections when item(s) are deleted. Delete all purple text before preparing the final document. All other modifications to this Section will require ODOT Technical Resource and State Specifications Engineer approval.)

Section 01013 is not a Standard Specification and is included for this Project by Special Provision.

## Description

01013.00  Scope - This Work consists of furnishing and installing a water quality bioslope as shown.

## Materials

(Delete material items that do not apply and include other materials as necessary.)

01013.10  Materials - Furnish Material meeting the following requirements:

Drainage Geotextile, Type 1	 02320

Facility Field Markers	 00842.10

Granular Drain Backfill Material	 00430.11

Shoulder Aggregate	 02640.10

Subsurface Drain Pipe	 00430.10

01013.11  Ecology Mix - Furnish an ecology mix composed of the following:

3/8" - No. 8 mineral Aggregate gradation meeting the requirements of Section 00680.

Horticultural grade perlite in a pelletized or granular form, meeting the following gradation:

Sieve Size	Percent Passing (by Weight)

No. 4	99 - 100

No. 18	30 max

No. 30	10 max

Agricultural grade dolomite lime in a pelletized or granular form, meeting the following gradation:

Sieve Size	Percent Passing (by Weight)

No. 8	80 min

No. 60	25 min

Agricultural grade gypsum consisting of Calcium Sulfate (CaSO4·2H2O) in a pelletized or granular form, meeting the following gradation:

Sieve Size	Percent Passing (by Weight)

1/4”	99 - 100

No. 20	20 max

Blend the mineral Aggregate, perlite, dolomite, and gypsum so that the mixture is composed of:

3 cubic yards of mineral Aggregate per 1 cubic yard of perlite

40 pounds of dolomite per 1 cubic yard of perlite

12 pounds of gypsum per 1 cubic yard of perlite

Mix the Aggregate, perlite, dolomite, and gypsum before delivery to the Project. Mix the materials in the presence of the Engineer. Provide at least 5 Calendar Days' notice to the Engineer before beginning mixing.

## Construction

01013.40  General - Construct water quality bioslope facility as shown. Perform excavation and placement work only when the facility area is dry. Do not stockpile excavated material in the facility area.

(a)  Laying Pipe - Lay the pipe according to Section 00445. Place pipe with perforations upslope.

(b)  Joining Pipe - Fasten pipes together with coupling fittings or bands as specified for the type of pipe used. Cap the upstream end of the pipe.

(c)  Inspection and Repair - Place the ecology mix only after the pipe is laid, joined, and inspected. Remove and reinstall or replace all pipe that is out of alignment, has settled, or is damaged at no additional cost to the Agency.

(d)  Compaction - After placing the ecology mix and shoulder Aggregate, compact by saturating with water.

01013.41  Facility Field Markers - Install field markers as shown and according to Section 00842.

## Maintenance

01013.70  Cleaning - Remove all accumulated sediment and debris before completing the facility.

## Measurement

01013.80  Measurement - No measurement of quantities will be made for Work performed under this Section. The estimated quantities of Materials are:

(Identify bioslopes by the Drainage Facility Identification Number (DFI). List each DFI separately. Obtain the DFI, the items, and the quantities from the Designer. Fill in all the required blanks. Delete items that do not apply. Copy and paste for multiple facilities.)

Bioslope __(DFI)__ Quantities:

Item	Quantity

Excavation	 ____ Cu. Yd.

Mineral Aggregate	 ____ Cu. Yd.

Perlite	 ____ Cu. Yd.

Dolomite	 ____ Lbs.

Gypsum	____ Lbs.

Crushed Shoulder Aggregate	 ____ Cu. Yd.

Drainage Geotextile, Type 1	 ____ Sq. Yd.

Granular Drain Backfill	 ____ Cu. Yd.

____ Inch Subsurface Drain Pipe	 ____ Foot

Field facility markers will be measured according to 00842.80.

## Payment

01013.90  Payment - The accepted quantities of Work performed under this Section will be paid for at the Contract lump sum amount for the item "Bioslope, _____".

The drainage facility identification number is inserted in the blank.

Field facility markers will be paid for according to 00842.90.

Payment will be payment in full for furnishing and placing all Materials, and for providing all Equipment, labor, and Incidentals necessary to complete the Work as specified.