## Slide 1
CONNECTING TO
COLLECTIONS
Textile
Preservation and Care

## Slide 2
Objectives
Understand the fundamental principles of textile care and preservation (i.e. object handling, proper storage techniques, storage considerations, etc.).
Ability to choose appropriate materials and techniques for textile display and storage needs.
Become aware of archival materials and their utilization with textile objects.
Become aware of fiber structure and composition.
Recognize the agents of deterioration.
Base program provided by Kathleen Daly

## Slide 3
Fiber Composition
Cotton
Wool
Linen
Raw Silk

## Slide 4
Important Terms
Textile: A term originally applied only to woven fabrics, but now generally applied to fibers, yarns, fabrics, or products made of fibers, yarns, or fabrics.
Fiber: Any substance, natural or manufactured, with a high length-to-width ratio and with suitable characteristics for being processed into fabric.
Yarn: An assemblage of fibers that is twisted or laid together as to form a continuous strand that can be made into a textile fabric.
Fabric: A flexible, planar substance constructed from solutions, fibers, yarns, or fabrics, in any combination.
Finish: Any process used to add color and/or augment performance of unfinished fabrics.

## Slide 5
Textile Characteristics
Fiber form
  Filament vs Staple
Source of the fiber
  Natural vs Man-made
  Mineral
Method of construction
  Yarn vs Fiber-based
  Woven vs Knit
Plain Weave
Knit

## Slide 6
Fiber Tree
Fibers
Natural
Man-Made
Cellulose
Fibers
(vegetable)
Protein
Fibers
(animal)
Modified
Natural
Polymers
Synthetic
Polymers
Misc
Fibers
(mineral)
Bast Fibers
Leaf Fibers
Seed Fibers
Wool
Cashmere
Alpaca
Silk
Flax (Linen)
Hemp
Ramie
Agave
Pineapple
Palm
Cotton
Kapok
Cellulose
Nylon
Polyester
Polyurethane
Asbestos
Glass
Metal
Protein
Viscose
Acetate-Rayon
Acetate
Casein (milk)
Ardil (peanut)
Rubber

## Slide 7
Cellulose (Plant)
Cotton
  Staple fiber
  Rigid and stiff
  Absorbent
  Weakened by light
  Susceptible to mold
Flax/Linen
  Staple fiber
  Lint Free
  Naturally contains wax
  Low elasticity, stiff
  Highly absorbent
  Weakened by light

## Slide 8
Protein (Animal)
Wool
  Sheep or goat fiber
  Staple fiber
  Weak
  Water repellant
  Highly absorbent
  Susceptible to light
Silk
  Filament fiber
  Smooth
  Very strong, unless wet
  Water repellant
  Very susceptible to light and environment
  Sometimes weighted

## Slide 9
Synthetics
Usually petroleum based
Includes modified natural polymers
  Milk
  Wood
  Cotton
Utilization of the spinerette to manufacture synthetics.

## Slide 10
Nylon
Filament or staple fiber
Highly elastic
Abrasive resistance
Very strong, weak when wet
Resistant to:
  Mildew
  Mold
  Moths
Susceptible to light

## Slide 11
Polyester
Filament, staple, fiberfill, and nonwoven
Strong
High abrasion resistance
Hydrophobic
Susceptible to pilling
Resistant to:
  Molds
  Fungus
  Moths
  Beetles

## Slide 12
Regenerated Cellulosic Fibers
Viscose-Rayon
  Staple and filament fiber
  Weak, weaker when wet
Acetate-Rayon
  Cellulosic fiber treated with salt (ester)
  Staple and filament fiber
  Weak, weaker when wet
  High luster

## Slide 13
Objects Handling: The Basics

## Slide 14
Important Terms
Preventive: Inhibiting deterioration from occurring.
Restoration: Returning an object to its original condition or state.
Conservation: All measures and actions aimed at avoiding and minimizing future deterioration or loss.
Degradation/Deterioration: Aesthetic or physical weakening, making a textile unsuitable.

## Slide 15
Code of Ethics
Show respect
  Research
  Plan
Do what is
  Within your means
  Reversible
Use archival materials
Document
  Photograph
  Condition and examination reports
Be safe
A repair causing additional damage and stress to garment.

## Slide 16
Where to Start
Wash Your Hands!
Gloves optional, but…
  Wash hands first
  Do not wear lotion
  Do not touch hair or face
  Keep washing hands
  Exception – always with sequins!
Remove jewelry, watches, scarves, etc.
Tie hair back

## Slide 17
Work Space(s) - Dos
Large enough to accommodate textile spread out flat
Covered table top
  Padded muslin top
  Blotter paper
  Acid-free tissue
Clean
Adequate lighting
Pencils only

## Slide 18
Work Space(s) – Don’ts
Food or drink
Ink
Rigid rulers or tape measures
Scissors/blades/pokey things
Adhesives
Animals

## Slide 19
Use Common Sense
Slow and steady
One object at a time
Its NOT to wear!!!
You are not Lennie. No stroking.

## Slide 20
Look Before Leaping
Fully analyze what needs support
  How many total parts are there?
  Are there any separate pieces?
  Is anything going to fall off?
  Is anything broken?
  Where is it heaviest?
Fully support the textile

## Slide 21
Carrying Methods
Cart
Box
Sling
Tray

## Slide 22
Supporting Objects
Pick up from the strongest area, not at
  Shoulders
  Sleeves
  Collar
  Handles
  Ornamentation
  Hold by sides or bottom, only

## Slide 23
Lastly…
Never set things on the floor
Don’t stack too high, if at all
Cover the object when done

## Slide 24
Agents of Deterioration

## Slide 25
Monitor, Clean, Proper Housing!
Environmental Conditions
  Light
  Pests
  Temperature - 70°C
  Relative Humidity - 50% RH
Mitigate pests
Custom storage solutions
  Support objects in their intended configuration
  Aid in providing safe handling and study
  Appropriate for the object
  Appropriate for the storage area
  +/- 5

## Slide 26
Categories of Deterioration
Physical
Environmental
Corrosion potential/reactivity
Photo deterioration

## Slide 27
Agents of Deterioration
Inherent Vice
Use
Soil
Pests
Light
Temperature and Relative Humidity (RH)

## Slide 28
Agent of Deterioration:
Inherent Vice
Structural/Chemical instability
Composite objects
Regular housekeeping
Hospice
Cause:
Mitigation:
Shattered silk

## Slide 29
Agent of Deterioration: Use
Wear
Handling
Display
Minimize use
Display in low traffic area
Store/Display on archival mounts
Do not stroke, wear, etc.
Cause:
Mitigation:

## Slide 30
Agent of Deterioration: Soil
Body oils
Perspiration
Atmospheric debris
Dust, dirt, droppings
Regular housekeeping
Vacuuming
Cause:
Mitigation:

## Slide 31
Agent of Deterioration: Pests
Rodent
Insect
Microbial (mold)
Regular housekeeping
Keep environments stable
Cause:
Mitigation:

## Slide 32
Agent of Deterioration: Light
Exposure to UV
Irreversible damage
Keep objects away from windows
50-200 Lux
Use filtration (UV) filters
Cause:
Mitigation:

## Slide 33
Agent of Deterioration: Temperature and RH
Ideal conditions
  70° (+/-5°)
  50% RH (+/-5%)
Avoid fluctuation
Avoid extremes
Do not store objects in attics/basements
Keep circulation of air
Environment:
Mitigation:

## Slide 34
Mitigation of Deterioration
Regular maintenance is key!!
  Monitoring
  Housekeeping
  Collections schedule

## Slide 35
Archival Material

## Slide 36
Important Terms
Archival: Used to describe a material or product that is permanent, durable, or chemically stable.
Acid-Free: Something with a neutral pH at time of manufacture.
Buffered: Treated with an alkaline reserve (buffering agent) during production to alter pH.
Unbuffered: Acid-free products that are neutral or slightly alkaline, but do not contain an alkaline reserve.
Polyethylene: An inert translucent thermoplastic.
Polypropylene: A stiff, heat-resistant, chemically stable plastic.

## Slide 37
Acid-Free Paper Products
100% cotton rag or lignin-free
pH neutral
Unbuffered
Types:
  Tissue
  Blotter
  Mat Board
  Blue Board
    Corrugated or solid
    Flat, box, or tube
  Glassine

## Slide 38
Cotton Fabrics
Lignin-Free
Archival
Reusable
Types
  Knit
    Display/Storage Mounts
  Flannel
    Display/Storage Mounts
  Muslin
    Slings, Garment Bags, Covers
  Twill Tape
    Labels, Handles, Ties
  Stockinette
    Padded Hanger, Sausages

## Slide 39
Plastics
Polyester
  Mylar: Clear, inert, insect, water and oil resistant
  Polyfill/Polybatting: Non-woven, inert
  Polyfelt: Non-woven, inert
Polypropylene
  Tyvek (Spun-bonded Olefin): inert, non-abrasive, pH neutral, insect, mold, dirt, water, oil, and chemical resistant
Polyethylene
  Volara: Inert
  Ethafoam: Inert
  Coroplast: Inert, insect, water, oil, and chemical resistant

## Slide 40
Marvelseal
Barrier
Aluminum foil
Heat application

## Slide 41
Choose Your Elements Carefully
Needle punch vs Thermal punch fiberfill
Non-mercerized cotton
100% cotton or polyester
Overall quality
Read the label. Contains no resins.

## Slide 42
Cleaning & Storage Preparation

## Slide 43
Before Beginning
Documentation
Photograph
Remove Foreign Matter
  Pins
  Staples
  Paper (labels, etc.)
  Packaging
    Store separately
    Discard
    Includes any paper removed

## Slide 44
Soiling and Staining
Foxing
Mold
Rust
Dirt
Bodily secretions
  Blood
  Sweat
  Oil

## Slide 45
Odor
Fungal
Mold

## Slide 46
To Clean or Not to Clean?
Is the soiling significant?
  Will cleaning remove this significance?
What is your end goal?
  Display?
What is its condition?
  Browning
  Brittleness
  Breaks in the fabric along seam, fold lines
  Rips or tears
How is the textile significant?
Is it worth the risk?

## Slide 47
Cleaning Methods
Airing out
Vacuuming
Wet cleaning
  Stain Treatments
Dry cleaning
  Harsh – Chemical process
  Aggressive – agitation and tumbling
  If you must, go prepared

## Slide 48
Air it Out
Use a sheet in the shade
  On the ground
  Over a rail fence
  Over several clotheslines
Do NOT use Febreze
  Contains bleaching agent
  Long-term effects still unknown

## Slide 49
Vacuuming
Removes loose particulate matter
  Aids wet cleaning
  See the difference
Materials
  Mesh screen
  Clean paint brush
  Dedicated collections vacuum
Method
  Lowest possible setting
  Dab, do not rub
  Left to right, up and down grid

## Slide 50
Vacuums
Suction control (variable speed)
Low setting
HEPA filtration
Micro-tools
Example: Miele Polaris canister vacuum.

## Slide 51
Making a Screen
Materials
  Window screening cut to a manageable size, app. 18“
    Wash screening twice before using (once with soap, once without)
  Twill tape or bias binding
  Sewing machine
Alternatives
  Cheese cloth
  Pantyhose
  Tulle

## Slide 52
Labeling

## Slide 53
Labeling Textiles – Materials
Cotton twill tape / Reemay / Tyvek
Pigma pen
White/natural colored cotton thread
Sewing needles
Sewing scissors

## Slide 54
Labeling Textiles – Location
Inside of a cuff
  Choose a side
Interior neckline
Reverse of lower proper left corner
NOT around buttons, ornamentation, delicate areas

## Slide 55
Labeling Textiles – Process
Stitch
  Tailors tack (preferred)
  Running stitch
No knots
Short sides or four corners

## Slide 56
Storage Solutions

## Slide 57
To Protect and Preserve
Disaster
  Flood
  Fire
Environmental factors
  RH
  Temperature
Physical damage

## Slide 58
Things to Avoid
Attics
Basements
Plastic containers
Wooden chests, closets, or shelves
Cardboard boxes
Plastic bags
Moth Balls
Newspaper
Overstuffing
Non-archival materials

## Slide 59
Location, Location, Location
Ideal
  Midlevel
  Shelved
  Closets
  Interior walls
Not Ideal
  Attic
  Basement
  Directly on the floor
  Exterior walls

## Slide 60
Dos Overview
Wash unbleached Muslin or cotton sheeting
Pad folds with acid free tissue/muslin
Keep stacks short
Regularly (every few month) refold the textile
  Fold in the opposite direction
Check container and its location every month
Check container contents annually for pests and damage

## Slide 61
Methods

## Slide 62
Object Housing
Wrapping
Interleaving
Rolled
Hanging
Flat
Enclosures
Supports and Mounts

## Slide 63
Considerations
Weight
Overall strength
Overall condition
  Areas of weakness
  Level of deterioration
Age
Construction
Elements
Color
Store like items with like items!

## Slide 64
Wrapping and Interleaving
Preferred:
Tissue
Muslin
Cotton sheeting
Photo-Tex
Alternatives
  Ethafoam
  Volara
  Reemay
  Tyvek
  Mylar

## Slide 65
Rolled
Archival tube
Non-archival tube
  Marvelseal
  Mylar
  Muslin or tissue
Not for multi-layered textiles
  Velvets and other piles
  Quilts

## Slide 66
Hanging
Padded hangers, only!
Dust covers
Like colors
“Breathing” room
Embellishments
NO KNITS!!!

## Slide 67
Flat Storage - Boxed
Coroplast or Blueboard
Stackable
Appropriate size
Sling
Interleaving
  Embellishments
  Very delicate
Folding
  Use minimal folding
  Pad folds

## Slide 68
Flat Storage: Shelving & Drawers
Metal
  Ethafoam
  Mylar
  Tissues
Line shelf
Sling/Easily removable
Interleaving
  Embellishments
  Very delicate
Cover when done

## Slide 69
Preparing for Flat Storage
Adequate workspace
Get help!
Create curves, not folds
“Fold” into thirds
Avoid:
  Patting
  Overstuffing
  Old fold lines

## Slide 70
Enclosures
Mats
Folders
Encapsulation
Frames
Provides support
Surface protection
Delicate objects

## Slide 71
Supports and Mounts
Determined by
  Object
  Storage need
  Display need
Simple
Easy to remove
Not stressful

## Slide 72
Considerations for Displaying Textile Objects

## Slide 73
Questions to Ask Yourself
What is its condition?
Special needs?
Where will it be displayed?
  Lighting
  Environment
    Public Space
Can any damage happen?

## Slide 74
Remember To…
Pad out folds
Create a barrier layer
  Acid-free tissue paper
  Mylar
  Cotton sheeting (washed)
Avoid displaying directly on:
  Plastic
  Cardboard
  Wood
Never use nails, pins or staples
Utilize indirect lighting

## Slide 75
Rotate
Regularly (every few month) refold the textile
Rotate
  Equal amount of time on display and off
  Every 6 months, max

## Slide 76
Environmental Conditions
Exhibit Barriers
  Air born pollutants
  Handling
Indirect Light
  Fades – especially blacks and browns of historical textiles
  UV filtration

## Slide 77
Take Aways
Do no harm
  If in doubt, do nothing
Work within your means
Ask for help
Keep hands clean
Wash textile-based supplies
  Neutral detergent
  Extra rinse
Maintain regular housekeeping
Maintain regular inspection schedule